## Slide 1: Proposal to EIC:
IR Magnets
Dr. Holger Witte
Associate Director, MIT Bates
3/11/2025
H. Witte, on behalf of MIT Team (Z. Hartwig, O. Hen, E. Ihloff, J. Bessuille, S. Chamberlain, R. Vieira, S. Smith, T. Golfinopoulos, …)
Notes: Maximum character recommendations:
Contact info: 145
Main title: 38
Secondary title: 100
Update all text fields with your relevant information.

## Slide 2: One should always start with a joke…
… but I don’t have one (at least a good one)
An interesting story will have to do
1980: problems with the Isabelle magnet
  Isabelle: 400 GeV Center of Mass energy
  Required field: 5T
  Only first magnet worked, others after 45 training quenches
The Bob Palmer Magnet (‘the Rebellion’)
  Alvin Tollestrup, Carl Goodzeit, Rick Fernow, Bill Sampson…
  $40k budget (Nick Samios)
  ‘Borrowed’ cable from FNAL
  Peter Marston, MIT: machining of tooling parts, cured stack of cable (a bill that was never paid?)

## Slide 3: Overview
Proposal
Challenges B0pF
New concept for B0pF
  Quenches
  Structural improvements
Workplan/Schedule

## Slide 4: Proposal
MIT takes responsibility for B0pF
  Design
  Detectors
  Cryostat
  Integration
  Testing
Manufacturing
  In-house or with industrial partner
‘Turn-key’ delivery

## Slide 5: EIC IR: Overview
Forward
Rear
IR location: IR6
Magnet Technology Challenges:
Crosstalk
Field/gradient requirements
Apertures
Each rectangle: required minimum aperture, not magnet size
Things are tight – Tapered CCT magnets to solve (some) of the issues
CCT Magnets: Q1ApR, Q1eR, B0ApF
Skew quads, vertical corrector

## Slide 6: B0pF Forward Spectrometer
Measures particles emerging from the breakup of the colliding hadrons
Only ~6m from IP
  Beams not very separated (crossing angle 25mrad)
Beams share magnet aperture
  Hadrons: 1.3T field
  Electrons: 14T/m gradient
Present implementation: combined function magnet
  Large aperture quadrupole; zero field axis shifted with dipole
Space constraints/large aperture
  Requires 2K
B0pF is essential for the forward side of the IR (beyond its importance for physics)
Courtesy of
K. Hamdi (BNL)

## Slide 7: B0pF – Initial Workplan
Re-evaluate design of B0pF
Present implementation is based large aperture quadrupole, which may not be ideal
  Preliminary studies show that a pure dipole could lead to a lower peak field
  Requires bucking coil for electron beam
Address structural and quench issues
  Larger cable
  Approach: wire in groove
  Individual turns supported by steel former
  VPI soldering technique, developed at MIT (PSFC)
    Used successfully for HTS, transfer concept to LTS
    (NbTi has a history of performance in soldered configurations)

## Slide 8: Statement of Problem
B0pF: large aperture, high field magnet
  Aperture: ~0.6m
  Bpeak, wire: 4.8T
  Stored energy: 800kJ
Direct wind technology limitations
  HFDW magnet trained to only ~1260A
    ~3.15T aperture field, ~80mm aperture
    (designed for 5.6T)
  Small cable (1.42mm dia)
  Stored energy: ~28kJ
Challenges direct wind
  mechanically ‘soft’ structure
  Large cable not possible (intrinsic limitation)
  Low current: quench protection issues

## Slide 9: B0PF Peak Field Calculation (energize hadron dipole and quadrupole in series with 1058A )

## Slide 10: B0PF quench simulation results 0.75ohm dump resistor /10ms quench delay/0.1V voltage threshold /3-loop protection circuits/no QP heater
10
~1.8mm
10
Wire spacing – transverse quench propagation velocity?

## Slide 11: B0pF – New Design
Based on pure dipole (CCT)
  Lower peak field on wire: 2T vs 4.7T
Larger Cable: 6.25mm2 vs 1.2mm2
  1.065mm strand, Cu:Sc 1.6
  7 strands
Quenches safely (70K, single dump resistor)
  20 ms delay
Margin: 50%
Energy: 400kJ vs 800kJ
Compensation concept
  Bucking coil – reduces field to mT
  Iron collar (also return yoke for quad)

## Slide 12: Addressing the Mechanical Issues
Direct wind technique:
  Voids are filled with fibre glass cloth
  Tension roving overwrap
  Fill with epoxy
Can this be supported better?
  Use same technique which was successful for 20T HTS large aperture magnet for fusion
  Wire in groove
  Key: vacuum pressure solder impregnation
  Peak IxB: 800 kN/m (B0pF: two orders of magnitude lower)
Restrict movement, avoid quenches

## Slide 13: What was the SPARC Toroidal Field Model (TFMC) Coil Project?
1. Developed REBCO conductor technologies (2017-2019)
2. Designed and built the TF model coil (2019-2021)
3. Built and commissioned the test facility
(2020-2021)
4. Achieved 20 tesla full performance test
(2021)
VIPER cables
NINT coils
Completed in ~4 years by MIT and CFS in partnership with our vendors

## Slide 14: The TFMC Project in one picture: magnet and test facility
The TFMC was designed and primarily fabricated (w/ external vendors) and assembled at MIT with REBCO procurement+ QA/QC and pancake winding at CFS

## Slide 15: The TFMC Project in one picture: magnet and test facility
15-ton gantry crane
Vacuum cryostat, 20 m3
Binary LN2/SHe current leads
Data acquisition & PLCs
50 kA, ±10 V Power supply
LN2 reservoirs feeding shields
TFMC
Turbo pumps with iron shielding
3-axis Hall sensors (“Teslameters”)
Fiber optic current monitor
Supercritical helium 600 W @ 20 K, 14 bar
Instrumentation harnesses
Cryocooler arrays and cryoabsorber
Cryo control racks and compressors

## Slide 16: The TFMC is a large scale 20 T no-insulation REBCO magnet
Nominal Design Parameter | Value
Number of pancakes | 16
Total turns | 256
Total REBCO tape | 270 km
Operating temperature | 20 K
Coolant type | Supercrit. He
Operating coolant pressure | 20 bar (max)
Operating terminal current | 40 kA
Peak magnetic field | 20 T
Peak IxB force on REBCO | 800 kN/m
Inductance | 0.14 H
Magnetic stored energy | 110 MJ
WP mass | 5,113 kg
WP current density | 153 A/mm2
WP + case mass | 10,058 kg
WP + case linear size | 2.9 x 1.9 m

## Slide 17: LL #3: REBCO has proven impressively resilient to vacuum pressure solder impregnation in VIPER cables and TFMC
VPI soldering was successfully developed for VIPER cables and for TFMC
Process results in acceptable solder-induced Ic degradation (~2-3%) for full-scale HTS conductors
Over 100+ VPI solder processes to date
  Adaptation to cables, coils, plates, …
VPI soldering REBCO is a critical enabler:
  Demonstrated stability against high IxB cyclic loads
  Enabled simple, robust, ~nΩ electrical joints
  Provides high levels of thermal stability
For B0pF: highest performance VPI solder to immobilize NbTi cable, allowing traditional insulation technique
HTS stack
Solder
Heat transfer
Current transfer (e.g. joints)
IxB load transfer
REBCO survive and enable high-quality solder with low-frequency, small voids over long lengths with excellent bonding to solve challenges in high-field magnets
Current sharing

## Slide 18: LL #4: VPI solder stabilized REBCO has survived high IxB loading, relevant axial strain, and thermal cycling
VIPER Cables: Consistent, stable Ic (<5% Ic degradation) after 1500 IxB cycles at 382 kN/m loading (all angles on REBCO stack) with ~0.3% axial strain and thermal cycles
TFMC: Negligible Ic degradation after fabrication and several IxB cycles at >800 kN/m (perp. to REBCO plane) (small, isolated damage in low-frequency solder voids)
REBCO operational performance at the tape- or stack-level to date exceeds what is required for high-field SC fusion cables/magnets.

## Slide 19: VPI Soldering

## Slide 20: Direct Wind - Coil Construction
Cross section drawing;
  Inner Helium Vessel (Coil Support Tube).
  12 layers of 6 around 1 superconducting cable (1.575mm dia.).
    Wound in pairs
    Each layer wound on B-stage substrate.
  Large gaps filled with 5 layers b-stage fiberglass cloth.
  Interstitial areas between conductors, filled with Stycast 2850 FT.
  Tension Roving added after each double layer (20lbs@ 18 turns/inch)
  .75mm thick layer of machined fiberglass (after each double layer).
  Outer compression sleeve (.1mm diametric interference fit with coil).

## Slide 21: CMS@LHC ETL Evaporators/Cooling Plates
Need very thin Al plates (6.35 mm thick /~ 3 m linear size)
Silicon detectors need to operate at -25C with good uniformity (1K)
Only 98mm space available
CO2 evaporative cooling
  Stainless cooling tubes
  Need excellent thermal contact: vacuum-bagged reflow soldering (adaptation of VPI process)

## Slide 22: LBNL: CCT Magnet
What are the chances of this working?
LBNL experience – Nb3Sn

## Slide 23: LBNL - CCT

## Slide 24: Why B0pF?
B0pF important not only for physics but also for machine
  Separation between beams
Standalone magnet
  Relatively easy to separate out
Combination with detectors – MIT can provide complete package
Not that sensitive to conductor placement
  Bucking coil wrecks havoc on field quality – sextupole (known)
  Large aperture

## Slide 25: Initial Work Plan
Conceptual EM Design
  B0pF: study dipole vs. quadrupole
    Fringe field
    Bucking coil for electron quad
  Basic quench analysis
  Margin/loadline
  Choice of conductor/cable
  Field quality
  Field map for physics
  Milestone: preliminary choice of design concept
Structural analysis
  Stress/strain analysis of typical direct wind magnet
  Stress/strain analysis of improved design

## Slide 26: Preliminary Schedule

## Slide 27: Open Issues/Questions
Collaboration
  EIC?
  Engage students
Construction
  In-house/industrial
  VPI process: MIT
VPI impregnation
  Insulated vs non
Measurement equipment
  No rotating coil setup
What does it take to make a small demonstrator?
  Fail fast, fail early
  MIT has capability to turn around prototypes fast, all in-house (including testing)
NbTi strand
  Preliminary design based on 1.065mm dia strand

## Slide 28: Magnet Technology at MIT - Expertise
Magnet design expertise
EIC IR expertise
Cryo expertise
Vacuum expertise
Structural mechanics expertise
Software
  COMSOL
  ANSYS
  Opera
PSFC
  VPI soldering technique
  Quench protection

## Slide 29: Magnet Technology at MIT – Facilities/Equipment
MIT Bates
  ~80 acres of land
  100,000 square feet of office and lab space
  12 MW of power available
  Power supplies
    2400A, 215kW PS
  Bates HPRC
PSFC
  Fabrication and VPI solder capabilities
  He Liquifier
    New Linde 70L/h cryoplant
    C.f. AUP magnet: needs 1000L (15000lbs)
  Superconducting magnet test facility (50 kA, 10V)
Various cryostats

## Slide 30: Things to discuss
Collaboration
Scope
  B0pF
  Direct wind machine for larger cable?
  Testing?
  Q1ABpF? (tapered quads)
  B0ApF?
Strand/cable
Next steps

## Slide 31: Summary
MIT: long experience in Magnet Technology
  Francis Bitter Lab, PSFC
  Peter Marston
  Bruce Montgomery
  20T all HTS fusion magnet
B0pF: challenging magnet, but MIT has the technology to make this work
  VPI soldering technique
  Larger cable to address quench issues
  Integration with detectors
Other opportunities?
Bates and PSFC: experienced team, eager to get to work
  Teams have a long history working together

## Slide 32: Additional Slides

## Slide 33: B0ApF
Requirements:
  Aperture: 120mm (coil)
  Length: 0.6m (magnetic length)
  Field: 3.3T
  (c.f. HFDW: 80mm aperture, max. 3.1T)
Same cable as B0pF
  Hot spot <90K

## Slide 34: Training Free CCT